## Slide 1: Microscopy of Clinker and Hydraulic Cements
Paul Stutzman
National Institute of Standards and Technology (NIST), USA
Paul.Stutzman@nist.gov
Clinker, HF-etch, 300 m FW
0.45 w/c, 7 d 30 m FW
0.45 w/c, 1 d, 50 m FW

## Slide 2: Historical Perspective
Calcined impure gypsum for mortar of masonry of Egyptian pyramids
Greek and Roman periods use calcined limestone with crushed brick, tile, and volcanic tuffs as they produced a superior product
While the volcanic ash-based cements worked, little was know about why they worked
John Smeaton construction of the Eddystone lighthouse (left) used a hydraulic cement he developed for the foundation
(1756)
Pont du Gard aquaduct at the top used a volcanic ash – lime binder to parge the walls

## Slide 3: Early Developments
1817 Erie Canal, used a Roman cement for mortar and stone construction
1821 Thomas Jefferson – utilized a Roman cement and natrual cements in the construction of his home in Montecello, VA.
1824 Joseph Aspdin, patent on Portland Cement
1850 David Saylor, Copley PA – first commercial production in North America
1883 Henri LeChatelier first applied the newly-developed petrographic microscope for clinker microscopy and the beginning of our understanding on the compositions and properties of hydraulic cements
1897 A.E. Toernebohm named the phases observed using the petrographic microscope: alite, belite, celite, felite
1908 Thomas Edison built a cement plant and developed cast in place concrete homes, many of which are still in use.
1912 NBS studies by P H Bates and A A Klein on composition and performance properties used the petrographic microscope to study the raw materials and hydration products
1934 B. Tavasci developed polished clinker microscopy that we use today
1
2
4
7
9
Thin section micrograph, crossed nicols, showing segregated large alite (gray) and fine belite crystals.
190x (original), P.H. Bates, 1917
8

## Slide 4
Portland Cement, Portland Stone
http://weymouthandportland.com
The name Portland was in reference to the appearance of the hardened portland cement concrete to the popular building stone of the day.
A North American equivalent to Portland Stone is the Indiana (Salem) Limestone, found in many buildings, including:
- Holocaust Museum, Washington D.C
- Empire State Building, New York
- Washington D.C. National Cathedral
- White House and Capitol repairs and expansion
www.visitingdc.com
Indiana Limestone, NIST Stone Wall collection (http://stonewall.nist.gov)

## Slide 5
P.H. Bates: 1910 – 1919 U.S. Government Specification for Portland Cement, later adopted by ASTM and in 1922 as the first American cement specification
Robert Bogue, Director of the Portland Cement Association Fellowship, NBS 1924 – 1954, The Chemistry of Portland Cement
Testing cements for Federal projects – large dam construction
Early studies on hydration products of cement phases and their role in durability
Cement performance studies – development of ASTM specifications and standard tests
Early XRD studies confirmed LeChatlier’s postulation of alite (Ca3SiO5) as a principal constituent of clinker
Subsequent XRD studies examined other clinker phases and, noting the relationship between intensity and concentration worked on quantitative XRD analysis
SiO2
CaCO3
CaO
5 CaO• 3Al2O3
3 CaO• Al2O3
Ca(OH)2
Fe2O3
Al2O3
1926: Early X-ray powder diffraction
As part of the NBS and Portland Cement Association Fellowship, work continued in developing improved understanding of clinker composition, hydration products, and the influence of both on concrete performance.
Some Milestones in Cements Characterization and Performance

## Slide 6: Cementitious Materials Characterization
Why Microscopy???
It remains an important instrument in the improved characterization of the phase types, chemistry, and reactivity and may be applied to
Cements
Supplementary Cementitious Materials
Hydration Process
Degradation process and products
  Direct means for phase compositional analysis whereas the indirect chemical analysis and transform via the Bogue calculations is inherently inaccurate.
    Microscopy
      Light microscopy for clinker petrography – qualitative and quantitative
        Point counting and image processing and analysis
      High-resolution secondary (topography), backscattered electron (composition), X-ray microanalysis (chemistry), and transmission (shape) imaging
      Image processing and analysis for extraction and measurement of features
    X-Ray powder diffraction
      Qualitative phase identification
      Quantitative phase analysis
      Real-time hydration studies and analysis of reaction product

## Slide 7: Clinker Microscopy
Field width: 500 µm
Field width: 100 µm
The microscope is a relatively rapid means to assess the clinker fabric for the cement manufacturer.
Petrographic analyses of clinker utilize descriptive terminology for phase assemblages, texture and fabric, similar to that in igneous and metamorphic petrology.
Clinker fabric is comprised of three features: phase association, texture, and structure.
Phase association refers to the types and amounts of the constituent phases in the clinker.
Texture stands for the size, shape, and distribution of the phases, and
Structure refers to potential grain orientation and the pore system.
Textural terms commonly used are euhedral (or idiomorphic) for well-formed crystals, subhedral for moderately well formed crystals, and anhedral (xenomorphic) for poorly formed crystals, along with descriptive terms like dendritic, lath-shaped, and amoeboid.
In addition to the individual phase descriptions, the phase distribution is an important reflection of the grinding, homogenization, and mixing of the source materials throughout the clinkering process.
Phases may occur as clusters with distinct boundaries, in clusters with a ragged boundary, and as clusters forming streaks across the clinker nodule. These modes of occurrence may vary widely across a nodule so care must be taken to examine large areas in the examination of clinker.
If the phase abundance is the primary goal for the examination, crushing the clinker should provide a more uniform specimen for examination. For cements, this is less of a problem as the grinding provides a degree of homogenization.
SRM2686 (upper image) shows a medium-grained, heterogeneous texture while SRM2688 (lower) is a coarse-grained, homogeneous texture with some decomposition of alite to belite along grain boundaries.

## Slide 8: Sample Preparation
Provides a clear definition of microstructure features without altering the sample with preparation-induced artifacts
  simplifies identification of constituents
  facilitates description of features
  eases interpretation
  The preparation processes are essentially the same for different materials – clinker, cement, fly ash, slag, cement paste, concrete: grinding using progressively finer grits then polishing with diamond pastes to remove the surface damage from the previous step
  Time spent preparing the sample properly is more than regained in the ease of description and interpretation of features !
Cement Clinker
Cement (ground clinker)
Hardened Concrete
Ideal surface – flat with well-defined phases, chip, and scratch-free

## Slide 9: Epoxy Embedding Techniques
I use two methods for embedding cement clinker, hardened concrete and cement paste specimens for examination: 1) solution replacement and 2) vacuum assist using dried specimens
Solution replacement involves replacing the pore solution with ethanol and then the ethanol with a low viscosity resin, followed by curing the resin. This results in an embedded specimen that has not been dried and experiences the shrinkage cracking associated with drying.
Vacuum-assist uses a low temperature dried specimen (105 °C) and a low viscosity resin that is immersed partially in the resin (leave a free surface to facilitate air escape) allowing the resin to be drawn into the microstructure by capillary action. This can then be further assisted by covering the specimen with resin and pulling a vacuum to remove air, followed by curing the resin.
Cement, fly ash, slag and other powdered materials are suspended in a viscous epoxy, adding enough powder to create a ball of material. The epoxy is then cured and the sample is ready for polishing.

## Slide 10: Fracture Surfaces
The focus will be on preparation and examination of polished specimens because they are better suited for quantitative microscopy.
Some question how representative a fracture surface may be since it is the path of the crack plane through the weakest portion of the material.
Fracture surfaces remain useful when used in conjunction with polished sections as the spatial resolution for SEM secondary electron imaging is better.

## Slide 11
Polished Sections:
Potting, Cutting, Grinding, and Polishing
Polished specimens are typically potted in an epoxy or resin, serving multiple purposes
  Fills voids to support microstructure
  Appears dark in SEM imaging (or could be stained for thin sections)
  Provides a specimen that is easily handled for the cutting and polishing
Cutting and Grinding expose a fresh surface, diamond blade slab or wafering saws are suitable. Cutting fluids may include alcohols (ethanol, isopropyl) or propylene glycol
Abrasives of 220, 400, 600, and 1200 silicon carbide removes damage produced by the previous grit. After the 1200 grit grind, the surface is smooth enough for polishing with the diamond pastes. (start with the finest grit possible to cut a planer surface)
Polishing removes the damage imparted by the sawing and grinding operations through use of a sequence of successively finer particle size diamond polishing pastes ranging from 6 m to 0.25 m, and a lap wheel covered with a low-relief polishing cloth.
The goal is to prepare a smooth, scratch-free, low-relief surface of particles surrounded and permeated by epoxy, presenting the ideal surface for SEM imaging and X-ray microanalysis

## Slide 12
ASTM C-457 specifies a
minimum surface preparation
to facilitate identification and measurement of the entrained air void system.
The lapped surface improves definition of all the concrete constituents.
This simplifies the petrographers tasks in describing the concrete constituents composition and texture.
Polishing using finer grits (like 1200) will result in a better-defined microstructure, perhaps necessary for viewing and measuring the finer-sized air void systems produced today.
(same field of view, two different preps)
1 mm
Saw-cut surface – too coarse
Lapped using 600-grit
silicon carbide
Stereo Microscopy Example: Poor vs. Good Surface conditions and feature definition

## Slide 13
Cut and lapped surfaces are not suitable for SEM imaging because of the substantial surface damage.
In the example, a cross-section of a saw-cut preparation (now epoxy
impregnated and polished) shows the depth of damage from a small lab diamond blade saw (≈50 μm).
Damage of the sample is due to cutting and subsequent drying
shrinkage-related cracking of the paste.
Epoxy embedding will stabilize the specimen while polishing will remove the surface damage that prevents viewing clean, unaltered microstructure (unaltered at the microscope resolution, that is)

## Slide 14: 0.50 W/C, 7-day Old Cement Paste: Saw-cut vs. epoxy & polish preparation
Map-view images of samples taken from the same core clearly illustrate the improved feature definition with the epoxy-impregnated, polished sections
CH
Aggregate
Pores
Inner- and outer-product C-S-H
AFm

## Slide 15
Tools for preparing concrete and concrete-making materials for petrographic analysis

## Slide 16: Materials
Item Purpose
Diamond blade slab saw large-sized sample slabbing
Diamond blade wafering saw cutting of thin (mm-sized) sections
Propylene glycol diamond saw cutting lubricant
Alcohol: 200 proof ethanol cutting lubricant, cleaning aid
Ultrasonic bath or probe specimen cleaning
Specimen jars and lids for replacement steps
Potting epoxies (medium and low viscosity) for powders and hardened pastes
Dye, blue or red, alcohol miscible to estimate alcohol replacement depth
Refrigerator epoxy storage
Vacuum chamber and pump vacuum impregnation
Drying / curing oven capable of at least 65 C
Glass plate (400 x 400 mm) smooth surface for grinding
Lapidary wheel grinding and polishing
Mold cups potting specimens
Aluminum foil (heavy duty) for forming odd-sized specimen molds
Mold release facilitates removal of specimen / epoxy
Diamond pen label engraving
Abrasive papers (silicon carbide) coarse to fine grinding, 100 to 600 grit
Polishing cloths (low-relief) for 6 m and finer polishing
Diamond paste for polishing 6, 3, 1, 0.25 m in non-aqueous suspension
Lint-free cloths specimen handling and cleaning
Compressed air specimen cleaning and drying
Vacuum dessiccators specimen storage

## Slide 17: Epoxies / Embedding Media
Epotek 353 ND*
Higher-viscosity (like honey)
2-component
high-temperature epoxy
Beam-stable for SEM
Works well for powders
*Certain commercial equipment or materials are identified to foster understanding. Such identification does not imply recommendation or endorsement by the National Institute of Standards and Technology, nor does it
imply that the materials or equipment identified are necessarily the best available for the purpose.

## Slide 18: Epoxies / Embedding Media
L.R. White Resin*
Ultra Low-viscosity (like water)
Retains low viscosity when refrigerated
Single component, low toxicity
Cure with accelerator or at 60 °C
Beam-stable for SEM
Works well for cement paste and concrete
Used in the biological community and is available from most microscopy suppliers. I use the hard grade as it polishes better.
*Certain commercial equipment or materials are identified to foster understanding. Such identification does not imply recommendation or endorsement by the National Institute of Standards and Technology, nor does it
imply that the materials or equipment identified are necessarily the best available for the purpose.

## Slide 19: Potting Powders
1
2
3
4
1) Cast Blanks
- cure overnight
2) Drill holes
3) Mix Powders to a modeling clay consistency for cements and slightly runny for fly ash and slag*
- Cure
4) Grind and Polish
5) Carbon-coat for SEM**
* Take a few drops of epoxy, blend in cement until it forms a thick paste. If it cracks and breaks on mixing, it is too dry.
** Carbon works best for SEM backscattered and X-ray imaging as it does not adversely affect signal intensity and contrast and will not interfere with X-ray signals of interest (for example, another popular specimen coating, Au characteristic X-rays overlaps those from S)

## Slide 20: Grinding - do as little as possible !
Dry grind to reduce the
possibility of softening the resin (L.R. White primarily), resulting in particle plucking.
Clean with a cloth or compressed air under a fume hood

## Slide 21: Polishing - 1200 grit and 6 um polish are critical in removing cutting and grinding damage!
The specimen is polished on the outer portion, and then cleaned of polishing residue in the center of the cloth. There are many different types of polishing cloths and plates, I use these cotton SEM cleaning cloths, which areused once and then discarded.

## Slide 22: Grinding & Polishing
Saw or grinding marks
** Cement grain cross-section **
Polishing removes the damage imparted by the sawing and grinding operations.
This stage involves use of a sequence of successively finer particle size diamond polishing pastes ranging from 6 m to 0.25 m, and a lap wheel covered with a low-relief polishing cloth.
Polish times are about 3 minutes per step using relatively high pressure. Longer polishing times seem to create rounded edges and grain relief.
This may be performed manually or, for greater sample throughput, using a semi-automated polisher.
600 grit
1200 grit
(not quite done)

## Slide 23: Final Polish Criteria
Over-polishing or using polishing cloths designed to impart grain boundary relief can lead to rounded edges,
This will adversely affect the BE and X-ray imaging and, subsequently, the image processing and analysis
Few scratches (on specimen)
Sharp corners
Well-defined phases
Minimal phase surface relief
No etching
Filled voids
No polishing media residue

## Slide 24: A Clean Surface is Necessary
Try to minimize entrapped air voids (they trap powder that will charge)
Sonication using isopropyl may be useful
Wiping the polished surface on a fresh polishing cloth saturated with isopropyl will remove stubborn polishing residue
Compressed gas to evaporate alcohol and remove surface dust
Acetone final rinse for a few seconds seems to leave a cleaner surface that is better able to hold the carbon coating
Charging is not always evident in BE imaging but can be seen in SE imaging.
Charging artifacts – bright ungrounded particles and dark surfaces that have repelled the electron beam

## Slide 25: Cements pose additional problems - grain plucking, differing phase hardness relative to the epoxy however, the thicker, harder epoxy has worked well.

## Slide 26: Clinker Polish
Most clinker microscopy is done using reflected light and a polished, etched surface. The left image is after the final polish and cleaning (isopropyl followed by acetone), and the right after etching (HF vapor).
The clean, flat crystal surfaces and sharp edges reflect a good polish.
Clinker and cement polishing progress may be followed by viewing larger grains using the reflected light microscope, watching for the point where the grinding pits disappear before proceeding to the 3 um and finer polishing stages.

## Slide 27: Etching - Clinker
Etching provides contrast between phases with inherently little contrast under reflected light. Campbell and the Hoffmanner clinker microscopy texts provide details.
The KOH-water etch darkens the aluminate phases while nital (1 % nitric acid in ethanol, isopropyl, or methanol) colors the silicates.
Water etch using a high-nap cloth is useful to highlight most phases, like HF but will lack the halo effect that identifies alkali sulfates.
HF etch works well, but the hazards of handling HF preclude its use in most facilities
KOH followed by nital
SRM 2688, HF, 250 um field width

## Slide 28
Alite Ca3SiO5 C3S 45-75%
Belite Ca2SiO4 -C2S 10-30
Aluminate Ca3Al2O6 C3A 1-15
Ferrite Ca2(AlxFe1-x)2O5 C4AF 0-20
Lime CaO C 0-5
Periclase MgO M 0-10
Arcanite K2SO4 KS
Thenardite Na2SO4 NS
Aphthitalite K3Na(SO4)4 K3NS4
Langbeinite K2Ca2(SO4)3 KC2S3
Gypsum CaSO4 2H2O CSH2
Bassanite CaSO4 0.5H2O CSH0.5
Anhydrite CaSO4 CS
C = CaO
S = SiO2
A = Al2O3
F = Fe2O3
f = FeO
S = SO3
M = MgO
N = Na2O
K = K2O
H = H2O
Field width: 500 µm
Field width: 100 µm
The application of the microscope and XRD have provided new insights on clinker composition and phase influences on performance. The systematic application of quantitative microscopy (and XRD) promises to provide newer insights, particularly with the more complicated hybrid cements in production today.
Clinker is not the relatively simple 4 phase mixture, as seen in the early microscopy studies, but is a more complicated mixture of 10 or more phases, some with polymorphic modifications. Cements (ground clinker with gypsum and limestone) have the additional calcium sulfate and calcium carbonate phases.
To simplify reference to the phases, a code using the first letter of the element is commonly used in cement chemistry, as shown to the right. Generally, a term like C3S indicates a pure tricalcium silicate, while the term alite reflects the impure with minor substitution of Mg, Al, S, K, and Fe. This is not universally followed however.

## Slide 29
Tricalcium silicate (Ca3SiO5) is the predominant phase in modern clinker, contributing about 40 % to 75 % of the bulk (by mass), and is responsible for the bulk of the early age (< 28 d) strength of hardened concrete. It is commonly called alite, referencing the impure form found in industrial clinker. Alite is one of the primary framework grains, exhibits a hexagonal cross section, occurs as euhedral to anhedral crystals, and may contain inclusions of other phases.
Dicalcium silicate (Ca2SiO4) is the second most abundant phase in clinker, contributing between 10 % and 30 % of the bulk (by mass), and occurring as one or more polymorphs, predominantly the beta and occasionally the alpha form. Pure dicalcium silicate is also called C2S, which may also use a prefix (, , ) to indicate the specific form; the impure industrial product is termed belite. Etched polished sections can expose the lamellar structure of belite
Tricalcium aluminate (Ca3Al2O6) comprises from 1 % to 18 % by mass of a clinker, and may be referred to as C3A for the pure phase or aluminate for the industrial phase. It can occur in one or more of three crystallographic forms dependent upon the amount of chemical substitution. The aluminates react rapidly, but contribute little to the cement strength.
Tetracalcium aluminoferrite (Ca2AlFeO5), or C4AF is found in concentrations between 5 % and 15 % by mass of clinker. The ferrite phase is a solid solution with variable Al2O3 / Fe2O3 ratios and does incorporate substituted Mg+2, Si+4, Na+1, and K+1 ions. Ferrite is highly reflective and unaffected by etchants commonly used.

## Slide 30
The aluminate and ferrite phases are part of a liquid phase in the clinker, forming a matrix linking the silicate framework grains. Their texture is influenced by the cooling rate; coarse-grained for slowly cooled and fine-grained for rapidly cooled clinker. The fine-grained varieties can be difficult to distinguish using a light microscope and the terms “undifferentiated” and “differentiated” matrix are common. White cement is manufactured from clinker characteristically devoid of C4AF. The iron and minor amounts of manganese in the ferrite phase in portland cement result in a strong coloration, imparting the typical gray color to the clinker nodules and to the cement.
Periclase (MgO) results from MgO in the limestone feed material. Clinker with MgO contents in excess of 2 % will generally exhibit some periclase. It is dispersed throughout the clinker, within and between silicate and matrix phases as equant crystals, but may also assume a dendritic morphology. Periclase is relatively hard and resistant to etching reagents, making it stand out in topographic relief, and readily identified in low to medium-magnifications as pink grains when rocking the focus above and below the optimum. Periclase exhibits slow reactivity, forming brucite (Mg(OH2)) with a substantial volume increase. In a hardened concrete, this volume increase may not be accommodated and the strain may result in cracking.
Free lime (CaO) may occur when the CaO:SiO2 ratio of the raw feed material is too high, the raw feed material is not homogeneous, or from over-sized limestone fragments. Free lime, like periclase, may hydrate after the cement paste has hardened, with an increased potential for cracking. Free lime readily hydrates upon exposure to humid air, converting to portlandite over a short time.
The alkali sulfates occur as a number of different mineral forms, the most common being arcanite (K2SO4) and aphthitalite ((K,Na)3Na(SO4)2). Less common are calcium langbeinite (K2Ca2(SO4)3), thenardite ((Na,K)SO4), and anhydrite.
Finally, the pore system will influence grindability, a significant source of energy consumption in cement production.
Ferrite (white) and aluminate (gray) in the clinker matrix
Field Width: 100 μm

## Slide 31
Gypsum (CaSO4·2H2O) is added to the clinker during the cement grinding process. Although the term gypsum is used, either through impurities in the raw material or due to dehydration in the grinding process, the actual mineral forms may include bassanite (CaSO4·0.5H2O, often called hemihydrate or plaster), and anhydrite (CaSO4).
The availability of sulfate ions affects the hydration reactions involving the aluminate phases to form ettringite preferentially to the AFm phases, the latter being responsible for the stiffening phenomena called flash set where, as the name indicates, the concrete mixture stiffens rapidly and becomes unworkable during placement and finishing. Another phenomenon, called false set, involves the hydration of bassanite to gypsum with a concomitant increase in the rheological properties. In contrast to flash set, this problem may be overcome with time and additional mixing.
Limestone is another common addition to cements at the 5 % level and between 6 % and 15 % for portland-limestone cements. European cement specifications allow for up to 35 % limestone
The discipline of clinker petrography has evolved to better understand the clinkering process, to evaluate process-related problems in clinker production, and to better relate clinker compositional and textural attributes to concrete performance.
Microscopic examination is a direct means of analysis, in contrast to the indirect Bogue calculations that transform a bulk chemical analysis into phase estimates. While quantitative microscopy is an ideal technique for clinker analysis in cement manufacturing, it is not widely used today due to the time requirements. It remains very useful as a rapid screening tool to evaluate clinker production through semi-quantitative assessment of microstructural features and their association with potential processing problems.
SEM-BE image of cement powder embedded in epoxy, cut and polished to provide a cross section of the particles.
Powders are much more difficult to examine using light microscopy due to the smaller particle size and the propensity for etchants to remove the smaller grains upon treatment.
Gypsum (calcium sulfate phases, G) appears dark and will be more easily seen with the addition of X-ray imaging.
Field width, about 250 μm on the long axis
< G

## Slide 32: Clinker Microscopy
Useful clinker microscopy texts:
D.H. Campbell (1999) Microscopical Examination and Interpretation of Portland Cement and Clinker, 2nd ed., Portland Cement Association, Skokie/IL
F. Hofmänner (1975) Microstructure of Portland Cement Clinker, Holderbank Management and Consulting, Ltd., Holderbank/CH
H. Insley and V. Fréchette, (1955) Microscopy of Ceramics and Cements, Academic Press, NY
A useful chart for interpretation of clinker textural features is provided by F. Hofmänner (1975).
Using the image of SRM 2686 above, with medium-grained silicates exhibiting heterogeneous distribution, coarse matrix, free lime content little to none reflects a heterogeneous raw mix, normal burning conditions and slow cooling
While point count procedures (ASTM C1365) may be used to quantify features, visual estimates remain a very useful tool in evaluating the clinkering process.

## Slide 33: SRM Clinkers
Three SRM clinkers
Selected as representative of the range of textures and compositions for North American clinker production
Informational data on bulk chemistry, making them useful in extending certain analyte calibration curves
Certified phase mass fractions based upon combined microscopy and XRD analyses
Random-stratified sampling of packaged clinker
16 data sets for XRD, 10 for microscopy
Separate operators for each method, working independently
XRD samples crushed to – 10 μm
SEM preparation of whole clinker fragments (roughly 3 mm) in epoxy, polished
Certified values a weighted average of replicated values for multiple samples and expanded uncertainty for 95 % coverage

## Slide 34: SRM 2686a
Intermediate in crystal size relative to the other SRM clinkers, and exhibits heterogeneous phase distribution and little free lime.
Alite occurs as subhedral to anhedral crystals approximately 30 m in size.
Belite occurs in large clusters with an approximate crystal size of 20 m.
The matrix is differentiated with a medium- to fine-grained lath-like ferrite, and fine-grained aluminate filling the inter-lath voids.
Equant periclase crystals up to 15 m are common throughout the microstructure and the
Alkali sulfate phases aphthitolite and arcanite are disseminated throughout the microstructure.
According to the Hofmänner [1975] diagnostic chart, the belite clusters may represent heterogeneity or over-sized silica grains in the raw mix. The fine-grained matrix indicates rapid cooling from 1300 ºC, and the slightly elevated belite content may reflect a slightly low CaO content.

## Slide 35: SRM 2687
Fine-grained clinker with abundant subhedral alite with a grain size of about 40 µm
Few belite clusters with rounded grains scattered throughout the clinker, and some diffuse free lime clusters
Alkali sulfates are common and dispersed throughout the clinker along grain boundaries
Matrix is very fine-grained, undifferentiated, although SEM imaging will show micrometer-scale ferrite in the aluminate
Free lime clusters are common
Abundant porosity and fine-grained silicates should make this clinker relatively easy to grind
Silicate and matrix textural features may be interpreted as a raw feed having a high CaO content or perhaps heterogeneous blending. The matrix is abundant, but poorly differentiated, indicating a rapid cooling.

## Slide 36: SRM 2688
Coarse-grained, homogeneous clinker with euhedral to subhedral alite up to about 150 m in size
Some fine-grained ferrite and belite inclusions within alite crystals
Well-dispersed, rounded belite of size up to about 40 m along with common fine-grained belite occurring as alite decomposition around crystal boundaries
Two distinct matrix textures: both well differentiated where ferrite occurs as either a coarse lath-like or a medium-grained dendritic form, aluminate occurs as fine-grained with the dendritic ferrite, and more lath-like with the coarse ferrite
Periclase is a minor component and is fine-grained and dispersed within the matrix.
Alkali sulfates are uncommon and reside within the matrix.
The coarse-grained nature of the clinker silicates may reflect a long residence time in the kiln above 1300 ºC, or a high maximum temperature. The coarse matrix may reflect a slow cooling. Clinker nodules may experience different thermal histories from the outer-portion relative to the core, especially if they are large. Examination of a wide cross section of particles may be necessary to be able to make definitive conclusions on a clinker.

## Slide 37: Quantitative Microscopy: Point Count Analysis
For composites consisting of randomly distributed, randomly oriented phases, the planar area fraction is an unbiased estimator of the volume fraction.
The Glagolev-Chayes method, referred to as the point count method, is perhaps the most widely used technique in quantitative mineralogical analysis when using a microscope, and is the basis for ASTM C 1356, Standard Test Method for Quantitative Determination of Phases in Portland Cement Clinker by Microscopical Point-Count Procedure.
This procedure utilizes a grid of points to sample the clinker polished section. Selecting a combination of eyepiece reticule and magnification in conjunction with the clinker crystal size to achieve spacing so as adjacent points ideally do not fall on the same crystal is a general rule and sampling in a regular pattern across the sample.
About 3000 to 4000 points on clinker phases are necessary to have reasonable counting statistics for the measurements and a duplicate sample is recommended.
Calculate mass percentages by multiplying the volume fractions by the density of the corresponding clinker phase and normalizing the totals to 100 %.
Single sampling field for SRM 2688 clinker with a hydrofluoric acid vapor etch and 9-point grid where six points fall on alite, and one each on belite, aluminate, and ferrite.
A number of sources of systematic and random error are present in any quantitative analyses, influenced by sample preparation, specimen polishing and etching, and operator experience in point counting and phase identification.

## Slide 38: Quantitative Microscopy: Point Count Analysis
A number of sources of systematic and random error are present in any quantitative analyses, influenced by sample preparation, specimen polishing and etching, and operator experience in point counting and phase identification.
A statement of uncertainty should accompany any measurement. Uncertainty analysis for each phase fraction estimate is based on counting statistics.
Assume a representative sample was collected and that the sample size was reduced using proper practice. The measurement uncertainty of the phase fraction is related to the number of points falling on the phase and the total number of points counted
Using the clinker data provided in Table 1 on four specimens counted to about 3100 points each where N is the total number of counts, n the counts per phase, and f is the inverse of the F probability distribution for (1 - , 2(N – n + 1), 2n), available from the F table or calculated through a spreadsheet function. The upper, p(n)u, and lower p(n)l, 95 % confidence bounds are calculated as: