## Slide 1: SEM Imaging Clinker and Cement
Paul Stutzman
National Institute of Standards and Technology (NIST), USA
Paul.Stutzman@nist.gov

## Slide 2: SEM Imaging
The scanning electron microscope provides sets of images suited for processing and analysis.
While the resolution of the BE image is roughly similar to that of the higher-powered light microscope objectives, the inherent contrast and uniformity of the backscattered electron and X-ray images makes it possible to perform image processing (feature extraction) and analysis (measurements) for quantitative microscopy.
SEM analysis is perhaps the only microscopic means to characterize fine-grained, multi-phase particles like cement, fly ash, and slag.
The cement grinding operation reduces the clinker nodules to a size distribution that spans from about 45 m to down to about 1 m, destroying the clinker crystal arrangements that are so useful for phase identification.
Light microscopy is of limited use because of the fine particle size and the potential for any etching operation to partially or completely dissolve the finer-sized particles. The multiple SEM phase and chemical imaging modes help overcome these limitations for qualitative and quantitative microscopy
The cross-section sampling is the most amenable to quantitative microscopy so polished sections will be used in the subsequent examples
Image processing and analysis used to quantify image features replicates the quantitative methods performed in the early days of microscopy when sketches of the fields of view were used to quantify features

## Slide 3: SEM Imaging
Polished sections using backscattered electron and X-ray imaging provide an image set like that of the early-day reflected light microscopy, with the advantage of being able to perform qualitative and quantitative chemical measurement and produce an image set amenable to image processing and analysis
Backscattered electrons (BE) are sensitive to phase chemistry, referred to as the compositional image, with brightness proportional to average atomic number
The backscattered electron coefficient, η, provides an estimate of relative brightness and is useful along with phase occurrence within the microstructure, shape and chemistry for identification.
< The three NIST SRM clinkers are from Type I cements, yet exhibit substantial differences in texture and composition

## Slide 4: SEM Imaging: X-Ray Microanalysis
X-rays are generated as a result of the interaction between the high-energy electron beam and the specimen.
The X-ray spectrum consists of the characteristic lines for each element present, represented by peaks on the spectrum, and a background of white radiation.
X-ray microanalysis may be used to identify and quantify chemical composition of phases that can be used to generate images of element spatial distribution. The latter capability is particularly useful for image processing as it enables a set of element spatial distribution images to be included in the image processing.
XR imaging is necessary for distinguishing between phases that have the same BE coefficient yet are compositionally distinct and for identification of phases that are not easily detected in the BE image; periclase and some alkali sulfates will appear dark, like voids.
Combining the XR and BE images allows a degree of phase discrimination that is not available from any single image.
Al X-ray image

## Slide 5: SRM2686a
SRM 2686a at low magnifications illustrates distribution of phases and porosity. Abundant alite, clustering of belite, a differentiated matrix comprised mostly of ferrite and some fine-grained aluminate, and uniform distribution of periclase is typical for this clinker.

## Slide 6: SRM2686a
SRM 2686a at higher magnification with belite inclusions in alite crystals, a differentiated matrix dominated by the ferrite phase, and both equant and dendritic (right image) periclase.

## Slide 7: SRM2687
SRM 2687 is a fine-grained clinker with abundant alite, some small nests of belite, variable porosity, and abundant, undifferentiated matrix.

## Slide 8: SRM2687
SRM 2687, higher magnification images begin to reveal details of the matrix, which consists of both a medium and fine-grained ferrite

## Slide 9: SRM2687
SRM 2687 matrix appears to be a mixture of medium-grained ferrite, massive aluminate and a web-like textured ferrite intermixed with the aluminate that was not apparent in light microscope imaging.

## Slide 10: SRM2688
A coarse-grained clinker with uniform phase distribution, no free lime, a medium- to coarse-grained well differentiated matrix, and occasional presence of periclase and alkali sulfates within the matrix and along grain boundaries.

## Slide 11: SRM2688
SRM 2688 at higher magnifications showing the belite and ferrite inclusions within alite, and a medium (left) and a coarse-grained (right), well-differentiated matrix.

## Slide 12: Quantitative Microscopy Using Image Analysis
Index Phase Pixels Area Fraction
1 Alite 142372 72.41
2 Belite 26800 13.63
3 Aluminate 7113 3.62
4 Ferrite 12977 6.60
5 Periclase 171 0.01
6 Arcanite 196 0.01
7 Void 6979 3.55
We want to make the computer “see” and measure features of the material
We assist through selection of a subset of the data that will provide phase identification
Image Processing: Manipulating images (combining, subtracting, smoothing) to uniquely identify each phase
Image Analysis: Quantify phase abundance and surface area

## Slide 13
Belite
Alite
Ferrite
Aluminate
Spot EDS analysis
The BE signal provides a high-resolution, high contrast image of the microstructure but needs the addition of some chemical data. The silicates and the matrix phases are chemically distinct, which will be used in conjunction with the BE image for phase segmentation

## Slide 14
Belite
Alite
Spot EDS analysis vs. X-Ray imaging
However, dwell time is too short to allow clear distinction
We need to optimize collection to enhance the distinction
- lower kV to enhance low energy X-rays
- high probe currents to maximize count rates
- slower scan rates to average out noise
- sum image frames to improve signal/noise
Clear distinction between phases is possible with the longer counting times used for quantitative X-ray microanalysis

## Slide 15
X-Ray Imaging Energy Windows
background
The intensity within a window across characteristic peaks (including background) is used to generate the images. The background can be a significant source of noise for low concentration elements, but we will establish criteria to reduce its influence.

## Slide 16: BE and XR images for SRM 2686a
Typically for clinker and cements, calcium, silicon, aluminum, magnesium, iron, potassium, sodium, and oxygen are the most useful X-ray images
A visual assessment is usually all that is needed to identify significant images necessary to extract the set of constituent phases.
An example may be seen with aluminate and belite having distinct chemical compositions, yet exhibit a similar backscattered electron coefficient. The BE image illustrates this with relatively large, rounded belite grains appearing at the same grey level as the matrix-phase aluminate.
However, belite contains appreciable silica while aluminate contains aluminum, so use of one or the other of the X-ray images will serve to distinguish these phases.
Similarly, the calcium sulfate addition (for cement) and the alkali sulfates are usually difficult to see given the high brightness and contrast of the BE image. The X-ray images Ca, S, K, and Na may be used to aid in their distinction

## Slide 17: BE and XR images for SRM 2686a
General Rules for Phase Distinction
free lime - bright BEI, strong Ca, rounded
ferrite – bright BEI, matrix, high iron, prismatic
aluminate – intermediate BEI, matrix, high Al
belite – intermediate BEI + little Al, rounded
alite – medium-high BEI, hexagonal shape, abundant
periclase – low BE, high Mg, equant to dendritic
alkali sulfate – high S + K (sometimes Na), occurs along grain boundaries
gypsum – low BE, high S, low K, Ca
calcite – low BE, stronger Ca
dolomite – low BE, stronger Ca, Mg
quartz – intermediate BE, high Si
kaolin – Al + Si
slag – angular, uniform grains, Si, Mg, Al
Want to use the fewest number of images to perform the segmentation
Example of merging images to discriminate phases follows in the next 5 slides:

## Slide 18
BE
Ca
Si
Al
Fe
Mg
Na
S
K
Set of SEM images collected simultaneously so they register (align) and ready for processing

## Slide 19: Alite Segmentation Example
The Old Way

## Slide 20: Combine Images – Image->Color-> Merge Channels
Assign images to color channels, check “Create Composite” and “Keep Source Images”, Select OK
This works best with 8-bit or 16-bit images and not RGB, as only the first color plane is used
This example used ImageJ, a public domain imaging code for all platforms: http://imagej.nih.gov/ij

## Slide 21: Low-Count Noise Will Affect The Analysis
If you see grainy images in a RGB display in ImageJ or Multispec, it can usually be traced to an un-clipped, low-count image such as Mg, K, or Na
ImageJ provides greater user input in the removal of the noise

## Slide 22: Image Processing: Process->Math->Subtract
noise and low concentration
Retain these data
Using the sliders provides a numerical value on the noise level
You may then subtract that value from the image pixels, or designate that value to be ignored within the Multispec processing
Mg
Mg: Processed

## Slide 23: BE – Mg – Al Combining images adds the X-ray image information, facilitating the discrimination of specific phases
In some cases, segmentation of alite, belite, aluminate, ferrite and pores is possible from only the BE image however, the gray contrast between belite and aluminate is not distinct enough.
The addition of the aluminum X-ray image provides that distinction as seen with the blue coloration ->
Periclase, having a low BE coefficient will appear dark, like the voids so the addition of the Mg image data (here in green) will highlight its location within the microstructure

## Slide 24: BE – S – Na - K
The addition of K, Na, and S provides distinction of alkali sulfates along pore walls and incorporated between and within silicates
For cements – provides distinction between alkali sulfates and calcium sulfates
Other combinations may be useful, but the combinations of BE with Mg and Al, and BE with S, Na, and K will highlight most phases.
In materials with small amounts of Na, or in this case, Na is redundant and is not necessary
Small amounts of Na may result in a noisier image – as 8 bit images are scaled to 256 levels
In this case, 16 bit TIF images retain the original X-ray counts rather than scale them to 255 gray levels based upon the highest intensity signal in each image

## Slide 25: BE – Si - Ca
Some combinations are redundant, adding little, or nothing to the segmentation.
Ca and Si actually make the distinction between alite and belite less clear than in the BE image
The relatively short dwell time does not provide a distinct difference between the silicates based upon Ca – Si ratios.
The BE image is vital for segmentation success. Some approaches focus only on the chemical data and are less likely to generate a clean segmentation.

## Slide 26: Segmented Image
Virtual 3-dimensional cement particles:
J. Bullard, NIST
Segmented image is indexed by phase for each pixel
ready for analysis of phase area fraction and surface area
This may be performed by counting pixels for each phase or via spatial correlation functions, which contain information on volume fraction and specific surface for each phase
input data for hydration model
generation of virtual 3-d particles after combining phase and surface area with tomographic images of particles

## Slide 27
Fly Ash Microscopy: Define mineralogical and textural characterization, along with particle size and shape analysis for performance prediction and improve classification schemes
Ca - Si - Al
Today: Bulk Chemistry - Class F (ASTM C618)
Characterize phase type, distribution, and volume,
Identify and quantify mineral and total glass,
Identify, quantify, and classify mineral and glassy phases,
Particle shape and size (X-ray CT and laser diffraction),
Determine the relative reactivity of the fly ash constituents,
Development of new standardized measurement practice,
Provide the basis for improved fly ash classification scheme.
25 µm
Tomorrow: Bulk Chemistry, Microscopy, X-Ray Powder Diffraction, Particle Size Distribution

## Slide 28: Aggregate- Catoctin Metabasalt, VA, alkali-reactive
Ca
Si
Al
Mg
Fe
Na
K
Ti
P
The same techniques may be applied to aggregates, cement paste, mineral admixtures, and concrete.
In this example, the slowly-reactive Catoctin metabasalt microstructure is characterized and ready for phase identification via chemistry and reconciling with the XRD data
Segmented image from 10 image inputs